## Slide 1: USTC-IME LGAD design and performance
Xiangxuan Zheng, May 13th
On behalf of USTC HGTD Sensor Group
University of Science and Technology of China

## Slide 2: Overview
Introduction
  HGTD (High-Granularity Timing Detector)
  USTC-IME 2.X LGAD
  Measured result of USTC-IME 2.X LGAD
  Radiation hardness
  On wafer/Large Array IV&CV
  Collected charge and time resolution from beta-scope
  Inter-pad gap distance by testbeam (fill factor)
  Inter-pad resistance and capacitance (checked for cross-talk)
Conclusion

## Slide 3: ATLAS HGTD project
LHC (Large Hadron Collider) → HL-LHC (high-luminosity phase of LHC) in 2028 → pileup vertex densities ↑
ATLAS (one of the 4 major experiments at the LHC at CERN) → upgrade its detectors
The HGTD (High-Granularity Timing Detector) is chosen for the ATLAS Phase II upgrade.
The time information be used as another dimension for identifying the hard-scattering vertex at the HL-LHC.
HGTD should withstand the non ionizing radiation levels throughout the HL-LHC operations.
  This determines sensors’ lifetime
Because of its good timing performance and radiation hardness, LGAD (Low Gain Avalanche Detector) has been chosen as the sensor.
3
Run-2
HL-LHC
Local pileup vertex densities at generator level
truth interactions in a single bunch crossing in the z–t plane
Position of the HGTD within ATLAS
ATLAS Detector in LHC

## Slide 4: Low Gain Avalanche Detector
LGADs are n-in-p silicon detectors containing an extra highly-doped p-layer (gain layer) below the n-p junction.
The high electric field in gain layer region will accelerate the drifting electrons and generate avalanches.
With a proper design of gain layer, the LGAD can achieve promising S/N and time resolution.
Designed parameters:
  Active thickness: 50 μm
  Pad size: 1.3 x 1.3
  Hit efficiency: > 95%
  Radiation tolerance: 2.5e15 , 1.5 MGy
1 LGAD pad
15x15 LGAD sensor

## Slide 5: USTC’s roadmap on LGAD R&D with IME
 | USTC-1.0 | USTC-1.1 | USTC-2.0 | USTC-2.1
Propose | First attempt | Improved the process technology, same layout as 1.0 | New layout, mainly for yield study and issues fix | Same layout as 2.0, fast iteration
Performance | Few sensors can work (VBD ~250V, VGL 40V) | ~30% can work (VBD ~300V) | > 99% small sensors and ~35% 15x15 sensors can work, GR leakage disappeared. VBD lowered (~100-170V). | >99% small sensors and ~35% 15x15 sensors can work. Better uniformity, VBDs in idea range (~150-240V). Performance verified in β/Laser/TB and individual institute (JSI)
Problem | Almost all sensors have large current (VBD < 10V) | Almost all sensors have large GR current | Too low VBD for some wafers. | 

## Slide 6: Design requirement and challenge
Characteristics of LGAD | Requirement | Test method
Radiation hardness | 1. Use c-factor to present the radiation hardness 2. Other parameters should meet the requirement at 2.5e15 irradiation fluence. | Measure CV at different fluences to calculate c-factor to present the radiation hardness
Yield |  | On-wafer IV test
Uniformity | < 5% for V@2µA | Large-Array IV&CV test
Collected charge | > 4fC | beta-scope test
Time resolution | < 40ps (start), < 70 ps (end of lifetime) | 
Fill factor | Inter-pad gap distance < 100 µm | Test-beam
Quality of the pad isolation | Inter-pad resistance > 1 GΩ | Inter-pad IV&CV test
Characteristics of LGAD | Requirement | Test method
Radiation hardness |  | Measure CV at different fluences to calculate c-factor to present the radiation hardness
Yield |  | On-wafer IV test
Uniformity | < 5% for V@2µA | Large-Array IV&CV test
Collected charge | > 4fC | beta-scope test
Time resolution | < 40ps (start), < 70 ps (end of lifetime) | 
Fill factor | Inter-pad gap distance < 100 µm | Test-beam
Quality of the pad isolation | Inter-pad resistance > 1 GΩ | Inter-pad IV&CV test

## Slide 7: Radiation hardness of LGAD
The BiOi generated after irradiation will reduce the effective doping concentration and detector’s gain.
The c-factor is used to describe LGAD’s radiation hardness (degradation rate of the gain layer).
The Ci + Oi -> CiOi would compete with Bi + Oi -> BiOi => Borons are protected!
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation
Collect charge vs radiation fluence

## Slide 8: Use VGL to calculate c-factor
-V curve
VGL
VFD
C-V curve
Use extrapolating line segments to extract VGL and VFD from CV.
Use the VGL at different fluences to fit the function and get the c-factor
VGL: gain layer depletion voltage
VFD: fully depletion voltage
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 9: Evolution of the c-factor from different vendors
c-factor measured with CV method on the most promising wafer (rad. hard) for each vendors’ run.
With the carbon in the gain layer, the USTC LGAD prototypes show promising radiation hardness compared to other vendors.
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 10: On wafer I-V
VBD: breakdown voltage
Production of large array sensors is a big challenge for process technology.
The VBD distribution is used to check the yield and uniformity.
Before irradiated, most sensors’ VBD are 150 ~ 240 V
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 11: IV&CV of irradiated 5x5 sensor
The uniformity of VGL and V@2µA is smaller than 1%, which meet the HGTD specification (5% for V@2µA)
VGL uniformity: 0.14%
V@2µA uniformity: 0.27%
W17@2.5e15
GR and all pads grounded
T: 20 ℃ for CV, -30 ℃ for IV
CV curve
IV curve
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 12: IV of irradiated 15x15 sensor
W13@2.5e15
W15@2.5e15
V@2µA uniformity: 3.36%
V@2µA uniformity: 2.8%
For the W13 and W15, the uniformity of V@2µA are both smaller than 5%.
GR and all pads grounded
T: -30 ℃
Step: 5.0 V
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 13: Collected charge and time resolution from Beta-scope result
The β-scope test for W17/W19 have been carried out at USTC and JSI.
The results show the W17/W19 LGADs’ can reach 50 ps and collected charge can > 4fC with bias voltage below 500 V after 2.5E15 fluences.
The result have fulfilled the radiation hardness requirement of HGTD.
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 14: Inter-pad gap measured by testbeam
Use a continuous 120GeV pion beam to hit the sensor.
The SPS testbeam show ~60 µm inter-pad gap for IP3 sensors.
Sensor | Bias (V) | IP measured (µm)
W19 2x2 IP3 | 155 | 59
 | 145 | 63
 | 135 | 65
W17 2x2 IP3 | 170 | 60
 | 160 | 59
 | 150 | 62
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 15: Inter-pad resistance
W17@2.5e15
Apply negative high voltage to sensor’s backside.
Apply 0 or 1 V to center pad, GR and other pads grounded.
Measure the current of other pads and get the current difference.
The current between two pads is lower than 1 nA which means that the resistance is larger than 1 GΩ. This means the sensors meet the HGTD requirement.
GR and all pads grounded
T: -30 ℃
Step: 5.0 V
The inter-pad resistance and capacitance is a in-direct measurement of the cross-talk influence. (Quality of the pad isolation)
1 nA
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 16: Inter-pad capacitance
Apply negative high voltage to sensor’s backside.
Measured the inter-pad capacitance between the center pad and the other pads.
After irradiated, the inter-pad capacitance can be smaller than 0.5 pF at appropriate bias voltage.
The test result of the inter-pad resistance and capacitance have showed the cross-talk won’t affect the sensor’s performance.
W17@2.5e15
Frequency: 1 kHz
VAC: 0.51 V
GR and all pads grounded
T: 10 ℃
Step: 1.0 V
Radiation hardness Yield Uniformity CC & Fill factor Pad isolation

## Slide 17: Conclusion
LGAD: a novel detector with good time resolution and high radiation hardness.
The USTC-IME V2.1 LGAD are well characterized in different test:
All parameters indicate they meet the HGTD specification.
The pre-production (USTC-IME-V3.0) is on-going with all changes adapted to the latest HGTD requirement.
Characteristics | Performance
Radiation hardness | c-factor of W17 can reach 1.23×
Breakdown voltage | 150 ~ 240 V @pre-irrad.
Large array uniformity | For 5x5, uniformity of VGL and V@2µA < 5% @2.5e15. For 15x15, uniformity of V@2µA < 5% @2.5e15
Inter-pad gap | ~60 µm gap @IP3 achieved
Time resolution | 35 ps @pre-irrad. , 50 ps @2.5e15
Collected charge | > 50 fC @pre-irrad. , > 4 fC @2.5e15
Inter-pad resistance | > 1 GΩ @2.5E15
Inter-pad capacitance | < 0.5 pF @2.5e15
Characteristics | Performance
Radiation hardness | 
Breakdown voltage | 150 ~ 240 V @pre-irrad.
Large array uniformity | For 5x5, uniformity of VGL and V@2µA < 5% @2.5e15. For 15x15, uniformity of V@2µA < 5% @2.5e15
Inter-pad gap | ~60 µm gap @IP3 achieved
Time resolution | 35 ps @pre-irrad. , 50 ps @2.5e15
Collected charge | > 50 fC @pre-irrad. , > 4 fC @2.5e15
Inter-pad resistance | > 1 GΩ @2.5E15
Inter-pad capacitance | < 0.5 pF @2.5e15

## Slide 18: Relative Paper
Radiation hardness characterization of low gain avalanche detector prototypes for the high granularity timing detector
Performance of LGAD sensors with carbon enriched gain layer produced by USTC
Performance in beam tests of Carbon-enriched irradiated Low Gain Avalanche Detectors for the ATLAS High Granularity Timing Detector

## Slide 19
backup

## Slide 20: CV&IV before&after irradiated
CV
20℃
un-irradiated
IV
-30℃
2.5e15
IV
20℃
un-irradiated
CV
20℃
2.5e15

## Slide 21
J.J. Ge, NIMA, 2021

## Slide 22
C.H.Li, NIMA, 2022

## Slide 23: Test-beam setup