## Slide 1: Composite NOL-CsI scintillator

## Slide 2: Recent upgrades on electronics
CSA + Optional (RC)2 shaping
Modified bandwidth to reduce the decay time of the trailing edge
晶体
前端板+APD
后前端板

## Slide 3: Small crystal tests – XEL test
Apply NOL on the crystal with spray gun
Significant transformation effect of the NOL

## Slide 4: Small crystal tests – Cosmic ray test
Very limited energy deposition due to the small size
L. Y. enhancement effect needs further investigation (with VIS sensitive PMT)
Reasonable trailing edge (No obvious slow component)

## Slide 5: Large crystal tests
Firstly demonstrated at USTC for system feasibility validation
Apply NOL on the crystal at SIC (5g per crystal)
Experiment schemes:
1. Bare CsI + Teflon
2. CsI + NOL (face 1) + Teflon
3. CsI + NOL (face 1,2,3) + Teflon
4. CsI + NOL (face 2,3) + Teflon
1
3
2

## Slide 6: Large crystal tests
Hard to control and monitor the film thickness (Need automation device)
The current film thickness on the crystal seems thinner than 50 um (the thickness achieved by the mayer bar)
Comparison with last years’ experiment at USTC:
Much larger crystal size
Much thinner film thickness

## Slide 7: Large crystal tests
Significant slow component in large crystal – contributes large to the CR-(RC)2 L.Y.
Consistent results with 10.1016/j.nima.2023.168173 (CSA L.Y.)
Reduced Delta L.Y. after applying NOL. No significant slow component in the waveform of Scheme 3,4
  Contribution from slow component reduced?
Scheme | CSA L.Y. | Ratio | CR-(RC)2 L.Y. | Ratio | Delta L.Y.
1 | 117 |  | 174.1 |  | 57.1
2 | 146.69 | 1.25 | 220.13 | 1.26 | 54.5
3 | 266.36 | 2.28 | 294.0 | 1.69 | 28.3
4 | 255.7 | 2.18 | 287.1 | 1.65 | 31.4

## Slide 8: Large crystal tests
Laser test on 20.12.30
Excite the pure CsI under its intrinsic excitation wavelength and around its emission wavelength
  297 nm laser induces strong slow component at vis wavelength
Setup | τ1 (ns) | A1 (ns*V) | τ2 (ns) | A2 (ns*V) | τ3 (ns) | A3 (ns*V)
ug | 8.2 | 12.2 | 25.7 | 2.2 | --- | ---
gg420 | 5.1 | 6.5 | 26.9 | 60.7 | 496.5 | 8.9
uggg | 8.1 | 0.2 | 19.2 | 0.03 | --- | ---
Setup | τ1 (ns) | A1 (ns*V) | τ2 (ns) | A2 (ns*V) | τ3 (ns) | A3 (ns*V)
ug | 6.0 | 227.5 | --- | --- | 404.9 | 3.8
gg420 | 5.1 | 10.8 | 153.6 | 56.3 | 531.1 | 438.8
uggg | 5.7 | 0.23 | 45.0 | 0.03 | --- | ---
241 nm
297 nm
Combined ratio of each component |  |  | 
Decay time (ns) | 6 | 30 | 500
Ratio (%) | 19.6 | 70.4 | 10.0

## Slide 9
NOL 9
NOL 34
NOL 53

## Slide 10: Large crystal tests
Only face 3 painted
1. CsI + NOL9 + Teflon
2. CsI + NOL34 + Teflon
3. CsI + NOL53 + Teflon
4. CsI + NOL53 + NOL53 + Teflon
Plan:
  New paining scheme
  Light collection uniformity & timing resolution
Scheme | CSA L.Y.
1 | 232.2
2 | 244.87
3 | 273.64
4 | 302.90
1
3
2